## Slide 1: Computational Study of MRAM Cells
Swapnil Barman

## Slide 2: Rectangular MTJ (Ni80Fe20/Al2O3/Fe) Cells of Varying Aspect Ratio: H applied along X-Axis
50x100x10nm 4000 Oe
100x100x10nm 3000 Oe
150x100x10nm 2000 Oe
200x100x10nm 2000 Oe
225x100x10nm 2000 Oe
250x100x10nm 1250 Oe

## Slide 3: Recangular MTJ (Ni80Fe20/Al2O3/Fe) Cells of Varying Aspect Ratio: H applied along Y-Axis
50x100x10nm 5000 Oe
250x100x10nm 5000 Oe
225x100x10nm 5000 Oe
200x100x10nm 5000 Oe
100x100x10nm 5000 Oe
150x100x10nm 5000 Oe

## Slide 4: Elliptical MTJ (Ni80Fe20/Al2O3/Fe) Cells of Varying Aspect Ratio: H applied along Y-Axis
50x100x10nm 5000 Oe
250x100x10nm 5000 Oe
225x100x10nm 5000 Oe
200x100x10nm 5000 Oe
150x100x10nm 5000 Oe
100x100x10nm 5000 Oe

## Slide 5: Elliptical MTJ (Ni80Fe20/Al2O3/Fe) Cells of Varying Aspect Ratio: H applied along X-Axis
50x100x10nm 5000 Oe
250x100x10nm 5000 Oe
225x100x10nm 5000 Oe
150x100x10nm 4000 Oe
200x100x10nm 5000 Oe
100x100x10nm 4000 Oe

## Slide 6: GMR and Magnetic Switching of Nanoscale Spin valve Cells

## Slide 7: Rectangular Spin Valve (Ni80Fe20/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 100 nm x 100 nm
Aij= 0, Current = 1 mA
Magnetic Field = ±1500 Oe
NiFe (10 nm)
NiFe (10 nm)
Cu (5 nm)
M
H (Oe)
H (Oe)
R (H)

## Slide 8: Rectangular Spin Valve (Ni80Fe20/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 200 nm x 100 nm
Aij= 0, Current = 1 mA
Magnetic Field = ±1500 Oe
NiFe (10 nm)
NiFe (10 nm)
Cu (5 nm)
M
H (Oe)
H (Oe)
R (H)

## Slide 9: Rectangular Spin Valve (Ni80Fe20/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 250 nm x 100 nm
Aij= 0, Current = 1 mA
Magnetic Field = ±1500 Oe
M
H (Oe)
H (Oe)
NiFe (10nm)
Cu (10nm)
NiFe (10nm)
R (H)

## Slide 10: Rectangular Spin Valve (Ni80Fe20/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 250 nm x 100 nm
Aij= 0, Current = 1 mA
Magnetic Field = ±1500 Oe, Pinning Field: 300 Oe
M
H (Oe)
H (Oe)
NiFe (10nm)
Cu (10nm)
NiFe (10nm)
R (H)

## Slide 11: Rectangular Spin Valve (Ni80Fe20/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 250 nm x 100 nm
Aij= 0, Current = 1 mA
Magnetic Field = ±1500 Oe, Pinning Field: 500 Oe
H (Oe)
H (Oe)
M
NiFe (10nm)
Cu (10nm)
NiFe (10nm)
R (H)

## Slide 12: Elliptical Spin Valve (Ni80Fe20/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 100 nm x 100 nm
Aij= 0, Current = 1 mA
Magnetic Field = ±1500 Oe
M
H (Oe)
H (Oe)
R (H)
NiFe (10nm)
Cu (5nm)
NiFe (10nm)

## Slide 13: Elliptical Spin Valve (Ni80Fe20/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 250 nm x 100 nm
Aij= 0, Current = 1 mA
Magnetic Field = ±1500 Oe
M
H (Oe)
H (Oe)
NiFe (10nm)
Cu (5nm)
NiFe (10nm)
R (H)

## Slide 14: Rectangular Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 50 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
H (Oe)
H (Oe)
M
Co (10nm)
Cu (10nm)
NiFe (10nm)
R (H)

## Slide 15: Rectangular Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 100 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
H (Oe)
H (Oe)
M
Co (10nm)
Cu (10nm)
NiFe (10nm)
R (H)

## Slide 16: Rectangular Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 150 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
R (H)
H (Oe)
H (Oe)
M
Co (10nm)
Cu (10nm)
NiFe (10nm)

## Slide 17: Rectangular Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 200 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
R (H)
H (Oe)
H (Oe)
M
Co (10nm)
Cu (10nm)
NiFe (10nm)

## Slide 18: Rectangular Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 250 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
R (H)
H (Oe)
H (Oe)
M
Co (10nm)
Cu (10nm)
NiFe (10nm)

## Slide 19: Rectangular Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 250 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±5000 Oe
MR
H (Oe)
H (Oe)
M
Co (10nm)
Cu (10nm)
NiFe (10nm)

## Slide 20: Elliptical Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 50 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
M
H (Oe)
H (Oe)
MR
Co (10nm)
Cu (10nm)
NiFe (10nm)

## Slide 21: Elliptical Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 100 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
M
H (Oe)
H (Oe)
R (H)
Co (10nm)
Cu (10nm)
NiFe (10nm)

## Slide 22: Elliptical Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 150 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
M
H (Oe)
H (Oe)
R (H)
Co (10nm)
Cu (10nm)
NiFe (10nm)

## Slide 23: Elliptical Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 200 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
M
H (Oe)
H (Oe)
R (H)
Co (10nm)
Cu (10nm)
NiFe (10nm)

## Slide 24: Elliptical Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 250 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
M
H (Oe)
H (Oe)
R (H)
Co (10nm)
Cu (10nm)
NiFe (10nm)

## Slide 25: Elliptical Spin Valve (Co/Cu/ Ni80Fe20) Cells of Varying Aspect Ratio: H applied along X-Axis
Lateral dimensions: 125 nm x 100 nm
Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
M
H (Oe)
Co (10nm)
Cu (10nm)
NiFe (10nm)
H (Oe)
R (H)

## Slide 26: Comparison between single and arrays of spin valve cells
Lateral dimensions: 125 nm x 100 nm; Aij= 0, Current = 1 mA, Co Anisotropy = 400000 erg/cm3
Magnetic Field = ±2500 Oe
M
H (Oe)
R (H)
Single
M
H (Oe)
R (H)
2 x 2
(s = 25 nm)
M
H (Oe)
R (H)
M
H (Oe)
R (H)
2 x 2
(s = 10 nm)
2 x 2
(s = 50 nm)